## Slide 1: Project Mechanical Recycling of Post-Consumer Mattresses
Filled products
Category
Ingrida
2020 07

## Slide 2
The average household keeps their mattress for 7 years before seeking out a replacement for it.

## Slide 3
1,5 million mattresses are collected for disposal in the Netherlands each year.
How many of them in the world?

## Slide 4
Is it possible to recycle?

## Slide 5
Photo source: https://sleeponlatex.com/blogs/news/14319429-100-places-to-recycle-your-old-mattress?utm_medium=Social&utm_source=Pinterest

## Slide 6
Foam can be shredded and used in floor cushions.

## Slide 7
The shredded foam pieces can be compressed and bonded together creating the
rebonded foam for chair pads.

## Slide 8
GOAL
Use mechanically recycled post-consumer foam in
filled products and decrease the filling cost

## Slide 9: WHY?
Reduce solid waste that goes to landfill
Save energy in production
Prevent pollution
Become independent on virgin resources
Lower price filling
Lower final product price
Be responsible and showing good
example

## Slide 10: HOW?

## Slide 11: Brainstorming: opinion, ideas, experience What additional requirements must be for post-consumer foam Available labs for making tests. Test new and recycled foam (for comparison) Regular foam samples from suppliers Pilot supplier for production of samples with regular and recycled foam.
Workshop with engineers

## Slide 12
RISK ASSESMENT
Chemical risk
Restricted substances might be in post-consumer mattress of different brands.
ACTION: More frequent tests should be performed.
Hygiene risk
Bacteria, viruses, mold, fungi, soil, dust, fats, organic debris.
ACTION: Cleanliness tests need to be performed to evaluate how well the foam
has been sterilized.
Quality risk
Same requirements must be fulfilled as virgin foam.
Radiant risk
The detectors must be installed in the recycling companies.

## Slide 13
RISK ASSESMENT
Chemical risk
Restricted substances might be in post-consumer mattress of different brands.
ACTION: More frequent tests should be performed.
How frequent?
TEST DESCRIPTION
1. General Requirements for all materials
Biocides of all kinds (formulation review)
Cadmium and its compounds
CMR substances categories 1 or 2 (on preparation or mixture, NOT finished product) (formulation review)
SVHC
Fragrance (formulation review)
Lead and its compounds
2.5 Polyurethane foam
2,4 Toluenediamine (2,4-TDA), 2,6 Toluenediamine (2,6-TDA), 4,4 Diaminodiphenylmethane (4,4-MDA)
Chlorinated hydrocarbon solvents
Chlorinated paraffins (SCCP)
Flame retardants
Total Antimony content
Organic brominated compounds (PBBs, PBDEs)
Chlorinated paraffins (SCCP)
TEPA (tris-(aziridinyl)phosphine oxide)
TDCP, TCEP & TPP (Tris(1,3-dichloro-2-propyl) phosphate), Tris-(2-chloroethyl) phosphate, Triphenyl phosphate)
Organotin compounds
Phthalates (18P)
MAT-0010

## Slide 14
RISK ASSESMENT
Hygiene risk
Bacteria, viruses, mold, fungi, soil, dust, fats, organic debris.
ACTION: Cleanliness tests need to be performed to evaluate how well the foam has been sterilized.
What tests to perform?
Test foam according to the down&feather cleanliness standard:
EN 12935 Cleanliness Requirements for Down & Feathers:
EN 1162 Oxygen Number
if Oxygen Number > 20 then
Microbiological State - Bioburden EN 1884 must be tested
Optional:
EN 1164 Turbidity
EN ISO 3071 pH Value
IDFL 30 - down & feather Odour test or
GB 18401 Textile Odor test
ISO 17226 Formaldehyde

## Slide 15
Quality risk
Same requirements must be fulfilled as virgin foam.
RISK ASSESMENT

## Slide 16: PROJECT RESULTS
Mechanically Recycled bonded foam from post-Consumer Mattresses were tested in Intertek.
Chemical tests according IOS-MAT-0010 and IOS-PGR- 0029 were performed.

## Slide 17
(9) Ash content (EN ISO 11358:1997, 70C) Pass

## Slide 18: Failed – Free Arylamines content – 2,4 MDA

## Slide 19: Failed – Organotin content – DBT and total

## Slide 20: PASSED - Flame retardants content

## Slide 21
PASSED – Phthalate content

## Slide 22: PASSED – Total Cadmium (Cd) and Total Lead (Pb) content

## Slide 23: PASSED – Chlorinated Paraffins Content and Ash content

## Slide 24: PASSED – 205 SVHC
…

## Slide 25
Photo source: https://geteasymove.com/blog/the-best-practical-ways-how-to-get-rid-of-mattress
Conclusions
Mechanically recycled bonded foam from post-consumer mattresses do not meet IKEA requirements described in IOS-MAT-0010.
  Failed – Free Arylamines content – 2,4 MDA
  Failed – Organotin content – DBT and total organotin
2,4 MDA and organotin can not be eliminated by mechanical recycling process from the foam
Hygienic tests were not performed as chemical tests failed
Mechanically recycled bonded foam from post-consumer mattresses can not be used in IKEA filled products
Financial part – 2700 Eur (tests, Retour Mattress visit in NL)